Table 1: Types of plastics, their properties and common uses.

| Symbols | Types of plastics | Common uses | Properties | Recycled into |
| --- | --- | --- | --- | --- |
|  | Polyethylene terephthalates | Soft drinks, water bottles, containers, salad dressing, biscuit trays and salad domes. | Clear, tough, solvent resistant, barrier to gas and moisture, softens at 80 ℃. | Pillow and sleeping bag filling, clothing, soft drink bottles, carpeting, building insulation |
|  | High density polyethylene (HDPE) | Shopping bags, freezer bags, buckets, shampoo, milk bottles, ice cream containers, juice bottles, chemical and detergent bottles, rigid agricultural pipe, crates. | Hard to semi-flexible, resistant to chemicals and moisture, waxy surface, opaque, softens at 75 ℃, easily coloured, processed and formed | Recycling bins, compost bins, |
|  | Polyvinyl Chloride (PVC) Plasticized Polyvinyl chloride PVC-P. | Cosmetic container, plumbing pipes and fittings, electrical conduct, blister packs, wall cladding, roof sheeting, bottles, garden hose, Shoe soles, cable sheathing, blood bags and tubing. | Strong, tough, softens at 80 ℃, can be clear, can be solvent welded. Flexible, clear, elastic, can be solvent welded. | Compost bin |
|  | Low density polyethylene (LDPE) | Refuse bags, Irrigation tubings, mulch film, cling wrap, garbage bags, squeeze bottles. | Soft flexible, waxy surface, translucent, softens at 70 ℃, scratches easily. | Bin liners, pallet sheets |
|  | Polypropylene (PP) | Microwave dishes, lunch boxes, packaging tape, garden furniture, kettles, bottles and ice cream tubs, potato chip bags, straws | Hard and translucent, soften at 140 ℃, translucent, withstands solvents, versatile. | Pegs, bins, pipes, pallet sheets. |
|  | Polystyrene (PS) Expanded polystyrene (PS-E) | CD cases, plastic cutlery, imitation glassware, low cost brittle toys, video cases/foamed polystyrene cups, protective packaging, building and food insulation | Clear, glassy rigid, opaque, semi-tough, soften at 95 ℃, Affected by fat, acids and solvents, but resistant to alkalis, salt solutions, Low water absorption, when not pigmented is clear, is odour and taste free. Special types of Polystyrene (PS) are available for special applications. | Recycle bin |
|  | Other | Automotive and appliance components, computers, electronics, cooler bottles, packaging | Includes all resins and multi-materials (e.g. laminates) properties dependent on plastic or combination of plastics | Recycle bins |

Source: [21].